## Slide 1
Institute of General and Inorganic Chemistry
National Academy of Sciences of Belarus
Ca-Mg phosphates as an effective sorbents of 60Co and 85Sr radionuclides
Dr. Andrei Ivanets

## Slide 2
The aim of this work was to study the efficiency of Ca-Mg phosphate sorbents based on dolomite for 60Co and 85Sr radionuclides removal from aqueous solutions depending on the electrolyte content in the wide range of pH.
OUTLINES
Preparation and characterization of Ca-Mg phosphate sorbents
Study of 60Co radionuclide removal
Study of 85Sr radionuclide removal
Efficiency of Ca-Mg phosphate sorbents towards 137Cs, 85Sr and 60Co in multicomponent solution
RadChem 2018 – the 18th Radiochemical Conference
13 – 18 May 2018, Marianske Lazne, Czech Republic

## Slide 3
SYNTHESIS OF CA, MG-PHOSPHATE SORBENTS
700°C
800°C
900°C
D-700
D-800
D-900
CaCO3 - MgCO3
MgO - CaCO3
PD-1
PD-2
PD-3
Na2HPO4
MgO - CaO
THE SCHEME OF OBTAINING SORPTION MATERIALS BASED ON DOLOMITE
RadChem 2018 – the 18th Radiochemical Conference
13 – 18 May 2018, Marianske Lazne, Czech Republic
Notes: Полностью скопировать слово в слово из статьи в ворд формате

## Slide 4
RadChem 2018 – the 18th Radiochemical Conference
13 – 18 May 2018, Marianske Lazne, Czech Republic
Fig. XRD patterns of sorbents PD-1 (1), PD-2 (2) and PD-3 (3)

## Slide 5
RadChem 2018 – the 18th Radiochemical Conference
13 – 18 May 2018, Marianske Lazne, Czech Republic
Table. Chemical composition of Ca-Mg phosphate sorbents
Sorbent | Content, mmol g-1 |  |  |  |  |  | Ca/Mg | (Ca+Mg)/P
 | Ca | Mg | NH4 | CO3 | PO4 | H2O |  | 
PD-1 | 3.91 | 1.99 | - | - | 4.93 | 17.39 | 1.96 | 1.20
PD-2 | 1.84 | 3.07 | 1.52 | - | 3.78 | 23.70 | 0.60 | 1.50
PD-3 | 5.27 | 5.09 | - | 4.65 | 1.56 | 7.78 | 1.04 | 6.65
Sample | Specific surface area, m2g-1 |  | Pore volume, cm3g-1 |  | Pore size, nm | 
 | Asp | ABET | Vsp.ads | Vsp.des | Dads | Ddes
PD-1 | 19 | 22 | 0.069 | 0.080 | 14 | 16
PD-2 | 49 | 54 | 0.182 | 0.238 | 15 | 19
PD-3 | 15 | 17 | 0.041 | 0.043 | 11 | 12
Table. Adsorption and textural properties of Ca-Mg phosphate sorbents

## Slide 6
RadChem 2018 – the 18th Radiochemical Conference
13 – 18 May 2018, Marianske Lazne, Czech Republic
Component | Concentration, g L-1 | 
Na+ | 15.39 | 10.77
K+ | 0.57 | 0.40
Mg2+ | 1.82 | 1.28
Ca2+ | 0.60 | 0.42
Cl- | 27.77 | 19.44
SO42- | 3.85 | 2.69
Total salt content | 50.00 | 35.00
Table. Composition of modeling seawater solution
Chart: (a)
| 0 | 5 | 15 | 35 | 50
PD-1 | 3.1988 | 2.6699 | 2.139 | 1.8461 | 1.7607
PD-2 | 4.3867 | 4.0338 | 3.7817 | 3.5752 | 3.5205
PD-3 | 3.5652 | 2.8454 | 2.6624 | 2.3213 | 2.2253
Chart: (b)
| 0 | 5 | 15 | 35 | 50
PD-1 | 75.7788 | 48.2385 | 21.4375 | 12.3215 | 10.2093
PD-2 | 97.9839 | 95.4546 | 92.3727 | 88.2785 | 86.7657
PD-3 | 87.099 | 57.8005 | 47.8739 | 29.5404 | 24.6778
Fig. Effect of salt content (Cs) on the distribution coefficient (a) and the degree of sorption of 60Co (b) at pH 8.0 ± 0.5

## Slide 7
Fig. Effect of salt content (Cs) on the equilibrium рН of solutions after contact with sorbents
(with stable Co(II))
Chart: (a)
| 2.08 | 3.01 | 4.0939999999999994 | 4.9269999999999996 | 6.01 | 7.78
PD-1 | 1.35 | 1.56 | 1.6 | 1.76 | 1.83 | 1.85
PD-2 | 1.78 | 3.38 | 3.51 | 3.4 | 3.34 | 3.58
PD-3 | 1.92 | 2.06 | 2.17 | 2.2 | 2.15 | 2.32
Chart: (b)
| 2.08 | 3.01 | 4.0939999999999994 | 4.9269999999999996 | 6.01 | 7.78
PD-1 | 4.22 | 6.76 | 4.59 | 9.62 | 12.04 | 12.32
PD-2 | 10.68 | 82.87 | 84.15 | 82.41 | 81.32 | 88.28
PD-3 | 13.75 | 18.58 | 22.65 | 23.4 | 22.14 | 29.54
Fig. Effect of рН of initial solutions (pHs) on the distribution coefficient (a)
and degree of 60Co sorption (b) at the salt content of 35.0 g L-1
RadChem 2018 – the 18th Radiochemical Conference
13 – 18 May 2018, Marianske Lazne, Czech Republic

## Slide 8
RadChem 2018 – the 18th Radiochemical Conference
13 – 18 May 2018, Marianske Lazne, Czech Republic
1 – Co2+; 2 – CoOH+; 3 – Co(OH)2
Fig. Forms of Co2+in aqueous solutions, calculated from constants of hydrolysis
Fig. Effect of рН of initial solutions (pHs)
at the salt content of 35.0 g L-1on the equilibrium рН of solutions without
60Co after contact with sorbents

## Slide 9
RadChem 2018 – the 18th Radiochemical Conference
13 – 18 May 2018, Marianske Lazne, Czech Republic
Fig. XRD patterns of PD-1 (1, 2), PD-2 (3, 4) and PD-3 (5, 6) after interaction with solution of Co(NO3)2(1.0 g L-1) without (1, 3, 5) and with seawater modeling solution(50 g L-1) (2, 4, 6)

## Slide 10
Chart: Cs (g L-1 )
| 0 | 5 | 15 | 35 | 50
PD1 | 29.13 | 11.5 | 3.93 | 2.61 | 6.97
PD2 | 84.17 | 42.19 | 34.65 | 26.36 | 21.42
PD3 | 55.36 | 16.54 | 17.57 | 7.19 | 6.82
Chart: Cs (g L-1)
| 0 | 5 | 15 | 35 | 50
PD1 | 205.73 | 65.6 | 20.52 | 13.46 | 37.64
PD2 | 2657.42 | 364.99 | 265.24 | 178.8 | 138.67
PD3 | 625.81 | 99.18 | 107.52 | 38.87 | 36.62
Chart: Cs (g L-1)
| 0 | 3 | 10 | 20 | 35 | 50
PD1 | 7.74 | 7.6 | 7.5 | 7.185 | 7.19 | 7.08
PD2 | 9.04 | 8.96 | 8.6 | 8.44 | 8.3 | 8.34
PD3 | 7.98 | 7.83 | 7.53 | 7.4 | 7.35 | 7.2
without sorb | 6.35 | 6.342 | 6.3 | 6.38 | 6.37 | 6.365
RadChem 2018 – the 18th Radiochemical Conference
13 – 18 May 2018, Marianske Lazne, Czech Republic
Fig. Effect of salt content Cs on the degree of sorption of 85Sr (a), distribution coefficient (b) and the рН changes of solutions after contact with sorbents (c).

## Slide 11
RadChem 2018 – the 18th Radiochemical Conference
13 – 18 May 2018, Marianske Lazne, Czech Republic
Chart: pHs
| 2 | 3 | 4 | 6 | 8.4700000000000006
PD1 | 3.015 | 5.535 | 8.17 | 8.104 | 2.61
PD2 | 6.19 | 23.557 | 22.51 | 24.924 | 24.434 | 26.3565
PD3 | 6.22 | 11.54 | 7.23 | 13.253 | 7.19
Chart: pHs
| 2 | 3 | 4 | 6 | 8.4700000000000006
PD1 | 15.59 | 29.96 | 45.215 | 44.34 | 13.465
PD2 | 33.22 | 154 | 145.309 | 166.2916 | 161.99 | 178.8
PD3 | 33.25 | 65.69 | 39.344 | 76.517 | 38.869
Chart: pHs
| 2 | 4 | 6.37 | 8
PD1 | 5.18 | 7 | 7.19 | 7.2
PD2 | 6.47 | 8.33 | 8.3 | 8.4
PD3 | 6.23 | 7.32 | 7.35 | 7.34
Fig. Effect of рН of initial solutions (pHs) with salt content of 35.0 g L-1 on the degree of sorption (a) and distribution coefficient (b) of 85Sr and on the рН changes of solutions after contact with sorbents (c).

## Slide 12
RadChem 2018 – the 18th Radiochemical Conference
13 – 18 May 2018, Marianske Lazne, Czech Republic
Table. Sorption properties of different materials towards strontium ions
Sorbents | m/V, g/mL | Competing ions / composition | Concentration, mol L-1 | State of strontium / concentration (mol L-1) | S, % | Sorption, mg∙g-1 | Kd, mL g-1 | References
HA (bioceramics) | 1/100 | Ca2+ / CaCl2 | 1 × 10-5 ‒ 1 × 10-2 | Sr2+ / 1 × 10-1 | ‒ | ‒ | 516 ‒ 5 | [21]
HA (for liquid chromatography) | 1/100 | Ca2+ / CaCl2 | 1 × 10-5 ‒ 1 × 10-2 | Sr2+ / 1 × 10-1 | ‒ | ‒ | 1885 ‒ 17 | [21]
HA (prepared by a wet chemical precipitation) | 1/100 | Ca2+ / CaCl2 | 1 × 10-5 ‒ 1 × 10-2 | Sr2+ / 1 × 10-1 | ‒ | ‒ | 42 ‒ 1 | [21]
HA (biogenic, amorphous) | 1/150 | Na+ / NaCl | 2 × 10-4 ‒ 2 | Sr2+ / 1 × 10-3 | 66.2 ‒ 44.9* | 8.7 ‒ 5.9 | ‒ | [20]
 | 1/150 | Ca2+ / CaCl2 | 2 × 10-4 ‒ 2 | Sr2+ / 1 × 10-3 | 76.1 ‒ 5.8* | 10 ‒ 0.76 | ‒ | [20]
HA (commercial nano-sized, crystalline) | 1/150 | Na+ / NaCl | 2 × 10-4 ‒ 2 | Sr2+ / 1 × 10-3 | 16.0 ‒ 9.9* | 2.1 ‒ 1.3 | ‒ | [20]
 | 1/150 | Ca2+ / CaCl2 | 2 × 10-4 ‒ 2 | Sr2+ / 1 × 10-3 | 27.4 ‒ < 0.15* | 3.6 ‒ < 0.020 | ‒ | [20]
HA (biogenic, amorphous) | 1/150 | Seawater / Na+ (0.450 mol L-1) Mg2+ (0.052 mol L-1) Ca2+ (0.009 mol L-1) | 90 % of salt content | Sr2+ / 1 × 10-3 | 17.5* | 2.3 | ‒ | [20]
HA (commercial nano-sized, crystalline) | 1/150 | The same | 90 % of salt content | Sr2+ / 1 × 10-3 | 1.6* | 0.21 | ‒ | [20]
Clinoptilolite | 1/150 | The same | 70 % of salt content | Sr2+ / 1 × 10-3 | 0 | 0 | ‒ | [20]
HA (low-crystalline) | 1/200 | Na+ / NaNO3, | 5 × 10-4 ‒ 5 × 10-3 | Sr2+ / 2 × 10-3 | 42.5 ‒40.5 | ‒ | ‒ | [18]
 |  | Ca2+ / Ca(NO3)2 | 5 × 10-4 ‒ 5 × 10-3 | Sr2+ / 2 × 10-3 | 37.6 ‒ 24.0 | ‒ |  | [18]

## Slide 13
RadChem 2018 – the 18th Radiochemical Conference
13 – 18 May 2018, Marianske Lazne, Czech Republic
Table. (continued)
Sorbents | m/V, g/mL | Competing ions / composition | Concentration, mol L-1 | State of strontium / concentration (mol L-1) | S, % | Sorption, mg∙g-1 | Kd, mL g-1 | References
HA | 1/250 | Ca2+ / CaCl2 | 5 × 10-2 | 85Sr / ~ 10 kBq mL | 10 | ‒ | 30 | [35]
Ca-Mg phosphate based on dolomite: |  |  |  |  |  |  |  | 
PD-1 | 1/250 | Ca2+ / CaCl2 | 5 × 10-2 | 85Sr / ~ 10 kBq mL | 12 | ‒ | 40 | [35]
PD-2 | 1/250 | Ca2+ / CaCl2 | 5 × 10-2 | 85Sr / ~ 10 kBq mL | 31 | ‒ | 110 | [35]
PD-1 | 1/250 | Na+ / NaCl | 1.7 × 10-1 | Sr2+ / 3 × 10-2 | 99.2* | 217.6 | ‒ | [41]
PD-2 | 1/250 | Na+ / NaCl | 1.7 × 10-1 | Sr2+ / 3 × 10-2 | 99.2* | 196.5 | ‒ | [41]
PD-1 | 1/500 | Modelling seawater: Na+ (0.468 mol L-1) Mg2+ (0.053 mol L-1) Ca2+ (0.011 mol L-1) | 14 ‒ 100 % | 85Sr / ~10 kBq mL-1 | 11.5 ‒ 7.0 | ‒ | 66 ‒ 13 | This work
PD-2 | 1/500 | The same | 14 ‒ 100 % | 85Sr / ~10 kBq mL-1 | 42.2 ‒ 26.4 | ‒ | 365 ‒ 179 | This work

## Slide 14
RadChem 2018 – the 18th Radiochemical Conference
13 – 18 May 2018, Marianske Lazne, Czech Republic
Fig. XRD patterns of PD-1 (a), PD-2 (b) and PD-3 (c) after aging in water without salt (1) and in solution modeling seawater with salt content 10.0 g L-1 (2), 35.0 g L-1 (3‒5) at pH 2 (4), 6 (1−3) and 8 (5).

## Slide 15
RadChem 2018 – the 18th Radiochemical Conference
13 – 18 May 2018, Marianske Lazne, Czech Republic
Fig. Effect of salinity on the lg Kd of 60Co (a) and 85Sr (b) radionuclides on Ca-Mg phosphate
sorbents (V/m=500 cm3/g)

## Slide 16
RadChem 2018 – the 18th Radiochemical Conference
13 – 18 May 2018, Marianske Lazne, Czech Republic
CONCLUSION
High effective Ca-Mg phosphates sorbents towards 60Со and 85Sr were synthesized.
Effect of sorbents phase and chemical composition, salinity and pH of solution were studied.
The highest sorption efficiency and selectivity was obtained for PD-2 sorbent.
The simplicity of Ca-Mg phosphates preparation and use of widely occurring natural raw material dolomite for their production give the scientific basis for industrial implementation of novel sorbents for treatment facilities.
The produced materials are promising for application in seawater and liquid radioactive waste treatment from 60Со and 85Sr radionuclides.

## Slide 17
Prof. Sillanpää Mika
Dr. Andrei Ivanets
Dr. Radkevich Artem
Dr. Shashkova Irina
OUR SCIENTIFIC TEAM
RadChem 2018 – the 18th Radiochemical Conference
13 – 18 May 2018, Marianske Lazne, Czech Republic
Dr. Kitikova Natalia

## Slide 18
Thank you for your attention!
www.igic.bas-net.by
Andreiivanets@yandex.ru
Tel./Fax: +375 17 2842712