## Slide 1: Radiochemical characterization for a decommissioning purpose at NRg: The case of Ion Exchange Resins
Radiochemical Conference,
13-18 of May 2018
Mariánské Lázně, Czech Republic
Patrick Haaß
Gaël Ménard
Tanja Tomasberger
18th of May 2018

## Slide 2: Content
Overview and strategy of NRG in radiochemical characterization
Approach and methodology for radiochemical analysis applied on the Ion Exchange Resins
Results and status of the project
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 3: The Netherlands, Petten
intro

## Slide 4: WASTE Characterisation
Context:
  Higher demand for nuclear waste characterization from regulator/public
  Waste Acceptance Criteria (WAC) not globally standardized
  Definition of needs not fully clarified
Requirements for waste characterization
  Fit storage facilities acceptance criteria (if established)
  Representative of the radionuclide content
  Nuclide selections for characterization
Example given of common waste
  Internal of NPP
  Ions exchange resins (IER)
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 5: ION EXCHANGE RESINS
Continuous clean-up of the primary circuit and of the water basin
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 6: Ion exchange resins
Existing storage/treatment solution
  Direct storage in containers
  Direct cementation
  Steam reforming (THOR process)
  Incineration  Ashes + Cementation
Requirement in all cases:
  Activities and dose
  Nuclide content
    Short-lived RN (Transport related): H-3; (S-35); Co-60; Ni-63; Sr-90; Cs-137
    Long-lived RN (Storage related): C-14; Cl-36; Fe-55; Tc-99; I-129; U; Pu
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 7: Characterization in a nutshell
Comprehensive information for:
-Transport
-Safe long-term storage
CHARACTERIZATION
Cost:
Minimalize
the amount of analysis
Representative:
(As much “data” as possible)
Time and/or
public pressure
ALARA
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 8: Constraint on Homogeneity
Inside one container (Presence of hot spots?)
In the different containers of a same batch
IAEA recommendation on homogeneity of a waste stream
(IAEA-TECDOC-1573)
“For stable waste streams, measuring one or more key nuclides and non-radioactive elements may be sufficient to check the homogeneity. For example, a simple and stable waste stream could be declared homogeneous if NDA measurements of 137 Cs and/or 60 Co made at different locations are within a 30% relative interval”
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 9: SAMPLING
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 10: OVERVIEW of the contingent
Batch | Total containers | Containers sampled | Container internal homogeneity check
2004 | 16 | 6 | Yes, on 2 containers
2009 | 19 | 5 | No
2010 | 9 | 4 | No
2011 | 10 | 8 | Yes, on 1 container
2012 | 19 | 9 | Yes, on 4 containers
2014 | 22 | 7 | No
2017 | 24 | 4 | No
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 11: Preparation: IER Application
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 12: Preparation - Digestion
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 13: Preparation - precipitation
Separation in two steps
Selective precipitation of Sr
Co-precipitation of Ni and Fe
 Purification
 Separation
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 14: Results: Homogeneity
Chart: Drum #
| 20151649 | 20151652 | 20151655 | 20151658 | 20151664 | 20151667 | 20151670
Average | 41.1 | 41.1 | 41.1 | 41.1 | 41.1 | 41.1 | 41.1
+30% | 53.43 | 53.43 | 53.43 | 53.43 | 53.43 | 53.43 | 53.43
-30% | 28.77 | 28.77 | 28.77 | 28.77 | 28.77 | 28.77 | 28.77
Co-60 | 46.7 | 43.5 | 40.3 | 41.7 | 43.3 | 41 | 31.2
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 15: Results : Recovery and selectivity
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic
Chart: Sr recovery in %
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12
Sr 1st measurement | 89.11 | 72.06 | 65.65 | 80.25 | 70.35 | 73.9 | 73.91 | 71.86 | 86.61 | 83.61 | 71.94 | 77.95
Sr 2nd measurement | 77.72 | 81.53 | 88 | 95.62 | 95.62 | 91.89 | 70.55
Chart: Sr activity in Bq/g
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12
Sr 1st measurement | 1.05 | 1.4 | 38.99 | 30.6 | 6.69 | 6.69 | 7.02 | 8.79 | 5.76 | 7.1 | 10.65 | 8.1
Sr 2nd Measurement | 5.41 | 4.91 | 6.25 | 6.58 | 6.14 | 6.29 | 2.06

## Slide 16: Results : Recovery and selectivity
Nuclides | Recovery range
Fe-55 | 45%-75%
Ni-63 | 75%-95%
Sr-90 | 65%-96%
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 17: OVERVIEW OF THE RESULTS
Batches analyzed: 7 different production
Amount of samples taken: 36 for homogeneity
15 for full analysis
Homogeneity proven: Yes, on 6 production
Anomalies detected: Yes, on 1 production
Analysis performed : Gamma
Beta (in-house):H-3; Fe-55; Ni-63; Sr-90
Beta (other labs): C-14; Cl-36; Tc-99
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 18: New challenges:
Pyrolyser for analyses of C-14 and H-3
Development of Cl-36 and I-129 methods
Development of Tc-99
Analysis of Cationic Resins
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 19: Conclusion
Developed analysis for IER
Result in agreement with other labs
Norm ISO-17025 accredited
Large applications of the characterization work:
  Internal of nuclear power plants (Low flux reactor in Petten)
  Historical waste (Legacy waste project at NRG)
  Third party waste/decommissioning projects
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 20
Thank you for your attention!
Any question?
Contact:
Patrick Haaβ; haass@nrg.eu
Gaël Ménard; menard@nrg.eu
Tanja Tomasberger; tomasberger@nrg.eu
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 21: NRG CAPACITIES
Unique structure at NRG:
Hot samples:
  5 concrete, 12 lead shielded hot cells for high active samples
  20 glove boxes for intermediate samples
  Radiochemistry laboratories
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 22: NRG CAPACITIES
Several Gamma detectors and LSC capable of handling range from high to low active samples
  Advanced separation methods allow full characterisation of higher active nuclides along with low active nuclides
TriCarb 3180 TR/SL LSC
Low level HPGe gamma spectrometry system
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 23: Measurement
Direct measurements:
  Total Alpha / Total Beta LSC Calibrated to a specific amount of resin
  Gamma spectrometry
Indirect measurements:
  C-14 and Tritium by LSC
After oxidative combustion and absorption of gas
  Fe-55, Ni-63 and Sr-90 by LSC
After precipitation and purification of sample
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 24: Preparation: Overall Approach
Gamma spectrometry : Direct measurement
Total Alpha and total Beta: Simple preparation
  RN: Adsorption on resins surface
   Gel media as scintillation cocktail
   Homogeneity for LSC
Gel
Immobilized resin beads
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 25: SAMPLING: Background
IER Beds are emptied after regeneration: Still consider a potential inhomogeneity in the activity
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 26: CHARACTERISATION DECOMPOSED
Measurement
Sampling
Repeatability
Preparation
Matrix
Analyte
Analysis
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 27: Example: Matrix issue
General approach:
C-14: absorption in Carbosorb / sodium hydroxide
H-3: absorption in nitric acid
Issue:
Absorption of gases produced during destruction
colouring of Carbosorb / capacity reduction of sodium hydroxide
H-3 forms no volatile species
 no absorption possible
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 28: Preparation(1/2): General plan
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic

## Slide 29: Preparation (1/3): RN specific approach
Goal: Transfer of RN from IER into solution
Two approaches:
Leaching:
  Pro: Lighter process
  Con: Uncomplete recovery of radionuclides content
Destruction:
  Pro: No loss of content
  Con: More complex matrix
   Preferred approach for full inventory
RadChem, 13th -18th of May 2018, Mariánské Lázně, Czech Republic